## Slide 1
Weekly Report
Date: 2020.05.08
Name: Dimas

## Slide 2
Summary of weekly report
Electrochemical test (half cell)
Key findings: Discover zinc metal diameter by experimental anaysis.
Done this week: ECD analysis

## Slide 3: Study of Zinc Foil Surface Area as an Anode for Aqueous Zinc-ion Battery (Experiment and ML Approach)

## Slide 4
XRD Analysis
The materials have hexagonal crystal system with space group P63/mmc. So, it is well matched with pristine zinc structure.
Zinc powder commercial is from Sigma-Aldrich, zinc foil is in OCV condition with 16 mm diameter, zinc paste made by Zn powder : KB : TAB = 6 : 3 : 3 mg, and zinc anode 50 cycles run in 2M ZnSO4 electrolyte.
In zinc paste anode, there are 4 peaks which did not indexed whose come from KB and TAB peaks element.
And then in zinc anode 50 cycles, the peak in 004 was not existed. It seems the Zn anode structure started changing after long cycling.

## Slide 5
ECD Analysis

## Slide 6
ECD Analysis
AM:KB:TAB = 3 : 1.5 : 1.5
Voltage range = 0.8–1.9 V
Electrolyte: 1M ZnSO4

## Slide 7
ECD Analysis
The 6 cell samples checked with 0.15 and 0.60 mA/g current rate in 3 mg of active material.
On the first discharge cycle, the best capacity identified in d = 13 mm. Otherwise, in 200 mA/g current density, d = 11 mm showed the highest capacity.
One distinct sloping voltage curves are observed in all variations. This observation will be checked in CV analysis. The slight increase in the capacity upon the initial cycle due to continuous electrode activation in all samples.

## Slide 8
Conclusion
Future plan
Machine learning analysis to compare with experiment result.
Compile cyclability data to process for ML.